## Slide 1: Vremenski razlučiva Raman spektroskopija kolektivnih stanja daleko izvan ravnoteže
Damir Dominko, V. Grigorev, V. V. Kabanov, J. Demsar
Institute of Physics Zagreb
University of Mainz

## Slide 2
Kolektivno stanje i parametar uređenja
Princip praćenja ultrabrzih procesa
Primjer: (NbSe4)3I
Rezultati jakih pubuđenja

## Slide 3: Kolektivna stanja
Obično modulirane strukture/superstrukture
Niska dimenzionalnost
α‑(BEDT-TTF)2I3
T. Ivek et al, PRL 104, 206406 (2010)
~0.8e
~0.3e
Lindhard response function at 0K
0
2kF
k
0
1
2
3
4
c
D=1
D=2
D=3
0
2kF
k
0
1
2
3
4
c
0
2kF
k
0
1
2
3
4
c
Notes: carge transfer salts
BEDT.. molecules

## Slide 4
Faza:
p/2
0
Parametar uređenja u potencijalu
D
F
0
D
F
0

## Slide 5: Praćenje ultrabrzih procesa
Komponente:
  Fononske: A, f, G, f
  Elektronske: A, G/t
http://www.nims.go.jp/ldynamics/en/
Raman
Time resolved
K0.3MoO3
(NbSe4)3I

## Slide 6: (NbSe4)3I
AFE
Pseudo- Jahn Teller
XRD at 128 K: length L splits in two: L and I
XRD at 30 K: length I becomes even shorter
- LLS-LIS-LSS transitions
P4/mnc - P421c - P4 space group transition
Notes: P4/mnc - P421c - P4
(D6_4h)-(D4_2d)-S1_4

## Slide 7: (NbSe4)3I

## Slide 8: (NbSe4)3I – efekt jake perturbacije
Vremenski ovisna frekvencija moda
- Red shift by DE
- Phonon energy recovery in tE

## Slide 9: (NbSe4)3I – 3 pulse experiments
SAMPLE
D
P
p
t12
t
P-p par - Raman proba
→ D-P-p set – vremenski razlučiva Raman spektroskopija

## Slide 10: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2
t12~∞
t12=0.2 ps
2.6 ps
5.5 ps
2.8 ps → 12 cm-1
Oscillatory traces vs. t12

## Slide 11: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2
2.8 ps → 12 cm-1

## Slide 12: (NbSe4)3I – 3 pulse experiments
0.1 mJ/cm2

## Slide 13: (NbSe4)3I – 3 pulse experiments
0.5 mJ/cm2

## Slide 14: (NbSe4)3I – 3 pulse experiments
1 mJ/cm2

## Slide 15: (NbSe4)3I – 3 pulse experiments
1.5 mJ/cm2

## Slide 16: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2

## Slide 17: (NbSe4)3I – 3 pulse experiments
4 mJ/cm2

## Slide 18: (NbSe4)3I – 3 pulse experiments

## Slide 19: (NbSe4)3I – 3 pulse experiments

## Slide 20: (NbSe4)3I – 3 pulse experiments

## Slide 21: Zaključak
Kalorimetrijski: 7 mJ/cm2 – grijanje za 500 K
Ravnoteža: Jahn Teller distorzija uništena
Izvan ravnoteže: distorzija očuvana i vremenski modulirana
Nagli skokovi faze za p na početku/kraju svakog perioda
Modulacija utjecaja pobude na potencijal među ionima

## Slide 22: Hvala na pažnji!

## Slide 23: (NbSe4)3I – dynamics at high perturbations
Time evolution of spectra at high fluencies
- Elektron-fonon vezanje promijenjeno u kratkom vremenu

## Slide 24: (NbSe4)3I – 3 pulse experiments
P. Kusar et al. PRB 83, 035104 (2011)
1T-TaS2

## Slide 25: (NbSe4)3I – 3 pulse experiments
1T-TaS2
+ damping, long pulses, long penetration depth
Analytic in t12!!
P. Kusar et al. PRB 83, 035104 (2011)

## Slide 26: (NbSe4)3I – 3 pulse experiments
R. Yusupov et al. Nat. Phys. 6, 681 (2010)
TbTe3

## Slide 27: (NbSe4)3I – 3 pulse experiments
R. Yusupov et al. Nat. Phys. 6, 681 (2010)
TbTe3
t12
Analytic in t12!!

## Slide 28: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2 0.25 mJ/cm2

## Slide 29: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2

## Slide 30: (NbSe4)3I – 3 pulse experiments
2 mJ/cm2

## Slide 31: (NbSe4)3I – high fluencies
Same CW power, different repetition
- resolving steady state heating

## Slide 32: Probing of ultrafast dynamics
Laser